## Slide 1
Course on Sulphur-based Wastewater Treatment
Resource Recovery
Guanghao Chen
Di Wu
Notes: For this chapter, we gather to discuss a topic of utmost importance in the field of wastewater treatment.
The transition from passive treatment to carbon- and energy-neutral treatment, while simultaneously recovering valuable resources.

## Slide 2: Introduction
Wastewater contains 50% of lost or wasted resources in a city, making a prime focus for resource recovery.
Sulphur conversion-based wastewater technology explores energy-saving strategies and methods involving the conversion of sulphur.
Notes: It is widely recognized that over 50% of lost or wasted resources in a city find their way into wastewater,
making it a prime focus for resource recovery efforts.
In our pursuit of sustainable wastewater treatment, it is crucial to explore energy-saving strategies and methods for resource recovery from processes involving the conversion of sulphur

## Slide 3: Introduction
Wastewater
Biogas
Sulphur conversion:
  Metal sulphide
  Elemental sulphur
  Biohydrogen
  Hydrocarbons
  Polyhydroxyalkanoates
Notes: Wastewater treatment holds immense potential not only in addressing environmental challenges but also in harnessing valuable resources that would otherwise be lost or wasted.
Through advancements in anaerobic digestion, the collection of biogas has been a practiced method for over a century, while the recycling of nutrients through land application of bio-solids has been a well-established practice.
Today, we will discuss the emerging opportunities to recovery metals, miners, metabolic intermediates (such as hydrogen, hydrocarbons and polyhydroxyalkanoates), in the rapid expansion of biological sulphur conversion technologies.
By incorporating these principles, we pave the way for a more sustainable future.

## Slide 4
Sulphur conversion-based resource recovery: metal sulphide

## Slide 5: Metal sulphides (MeS)
MeS play a crucial role in several Industrial processes
  e.g. fuel refineries, hydro-processing, fuel cells
Nanoscale MeS take on even more significance
  e.g. cancer therapy, photocatalysis, optoelectronics, antimicrobial agents
fuel refineries
hydro-processing
fuel cells
photocatalysis
cancer therapy
optoelectronics
antimicrobial agents
Notes: Metal sulphides play a crucial role in several industrial processes, including hydrocracking in fuel refineries, hydro-processing, and oxygen reduction in fuel cells.
At the nanoscale, metal sulphides take on even more significance.
They find applications in cancer therapy, photocatalysis, optoelectronics, and as antimicrobial agents.
These emerging fields utilize the unique properties of metal sulphides to address important challenges in healthcare, energy, and materials science.

## Slide 6: Commercial MeS
Metal sulphides are generally synthesized through methods including:
        high gravity
        chemical baths
        γ radiation
        pyrolysis
        thermolysis
High temperature and pressure are essential
Use hazardous chemicals
Sources:
Huerta-Flores et al., 2018. J Mater Sci: Mater Electron 29, 11613–11626.
Sivakumar et al., 2017. Journal of Colloid and Interface Science 490, Pages 719-726
Notes: Commercial metal sulphides are typically synthesized using various methods such as high gravity, chemical baths,gamma-radiation, pyrolysis, and thermolysis of metal complexes.
These processes often involve high temperatures and pressures, and some may even use hazardous chemicals.
It's important to note that these synthesis methods require careful consideration and adherence to safety protocols due to the use of hazardous chemicals and the conditions involved.

## Slide 7: Bio-produced MeS
The biological production of metal sulphides is a safe, cost-effective and environmentally-friendly synthesis method.
  For instance, cadmium sulphide (CdS) nanoparticles can be intracellularly synthesized by photosynthetic bacterium Rhodopseudomonas palustris and E. coli are also capable of producing intracellular CdS nanocrystals.
Sources:
Zhang, L., et al., 2011. Journal of Nanoscience and Nanotechnology, 11(3), 2202-2207.
Song, J. Y., et al., 2005. Angewandte Chemie International Edition, 44(14), 2154-2157.
Rhodopseudomonas
H2S
Cd2+
CdS
Notes: In contrast to conventional methods, the biological production of metal sulphides offers a safer, more cost-effective, and environmentally-friendly synthesis approach. One remarkable example is the intracellular synthesis of cadmium sulphide (CdS) nanoparticles by certain microorganisms.
For instance, the photosynthetic bacterium Rhodopseudomonas palustris has demonstrated the ability to produce intracellular CdS nanocrystals.
Additionally, Escherichia coli (E. coli) has shown its potential in intracellular production of CdS nanocrystals within the size range of 2-5 nm.
These biological approaches utilize the natural metabolic processes of microorganisms to synthesize metal sulphides, providing a sustainable and eco-friendly alternative to traditional chemical synthesis methods.
By harnessing the unique capabilities of microorganisms, we can explore the potential for bio-inspired and bio-mediated synthesis of metal sulphides, unlocking new possibilities for nanotechnology and sustainable materials research.

## Slide 8: Bio-produced MeS
Sulphide is the product of sulphate reduction mediated by SRB, which can extracellularly bind to or precipitate with metal ions in solution.
Valuable metal sulphides produced via the metabolic pathway of SRB.
Notes: Now, let’s also look at the topic of metal sulphides and their production through the metabolic pathway of sulphate-reducing bacteria (SRB).
SRB play a crucial role in the reduction of sulphate to sulphide. This metabolic process results in the extracellular binding or precipitation of metal ions in solution, leading to the formation of valuable metal sulphides.
As we can see from the table, various metal sulphides are produced through the metabolic pathway of SRB.
For instance, copper sulphide (CuS) is one such valuable metal sulphide produced through this pathway. It is known for its applications in various industries, including photothermal agents for the ablation of cancer cells. The extracellular location and operational pH of 6.0 make it a promising candidate for medical applications.
Another example is cadmium sulphide (CdS), which is commercially important as a semiconductor material. The intracellular synthesis of CdS nanoparticles by certain microorganisms, as highlighted in the table, opens up possibilities for applications in solar cells, and sensors.
These examples demonstrate the versatility and potential applications of metal sulphides produced via the metabolic pathway of SRB.
In conclusion, the metabolic pathway of sulphate-reducing bacteria offers a sustainable and environmentally-friendly approach to the production of valuable metal sulphides.

## Slide 9: Strategies of MeS production
Two strategies are executed when SRB are applied in metal sulphide production:
In-line system: The metal directly reacts with the sulphide in the sulphidogenic system.
Off-line system: Sulphide is produced and separated as a metal precipitant agent.
Figure source: Hydrometallurgy 213, August 2022, 105950

## Slide 10: In-line system
Advantages
Biological-based synthesis demonstrated superiority in products stability – for example, the zinc sulphide (ZnS) precipitates biogenerated by Desulphovibrio sulphuricans are more stable than the abiotic ZnS precipitates.
The biogenic Ni3S2 in a mixed culture of SRB exhibits a better crystallinity than the corresponding abiotic samples (Gramp et al., 2007).
Disadvantages
The adsorptive extracellular polymeric substances, such as carboxyl, thiol/phosphate, and amino/hydroxyl of SRB and other organisms obstruct the formation of metal sulphides.
Aggregation induced by metal-binding polypeptides and proteins of organisms in an in-line system limit the dispersal of metal sulphide particles in the solution, reducing the potential to harvest those particles.
Soutce: Gramp J.P., Bigham J.M., Sasaki K. and Tuovinen O.H. (2007). Formation of Ni-and Zn-sulphides in cultures of sulphate-reducing bacteria. Geomicrobiology Journal, 24(7-8), 609-614.
Notes: Biological-based synthesis has shown its superiority in terms of product stability. For example, the zinc sulphide (ZnS) precipitates generated by the bacterium Desulphovibrio sulphuricans are more stable compared to abiotic ZnS precipitates.
Furthermore, studies have revealed that biogenic Ni3S2, produced in a mixed culture of sulphate-reducing bacteria (SRB), exhibits better crystallinity than the corresponding abiotic samples.
On the contract
The presence of adsorptive extracellular polymeric substances, such as carboxyl, thiol/phosphate, and amino/hydroxyl, produced by SRB and other organisms, plays a crucial role in obstructing the formation of metal sulphides.
Additionally, aggregation induced by metal-binding polypeptides and proteins of organisms in an in-line system limits the dispersal of metal sulphide particles in the solution, thereby reducing the potential to harvest these particles.

## Slide 11: Off-line system
Harvesting biogenic metal sulphides from sulphidogenic off-line system could be a suitable option, particularly in the treatment of metal-containing wastewater.
pH control is crucial for metal sulphide formation, since the binding characteristics of metals are also sensitive to pH changes.
For example, the nature, surface, and settling characteristics of CuS and ZnS are heavily influenced by the bulk pH (Mokone et al., 2010).
    For instance, with pH below 3, Cu can be selectively precipitated by sulphide.
    When precipitation is conducted with excessive sulphide at operational pH below 6, the zeta potential reduces to improve the settling and dewatering properties of ZnS precipitates.
Source: Mokone et al. 2010. Effect of solution chemistry on particle characteristics during metal sulphide precipitation. Journal of Colloid and Interface Science, 351(1), 10- 18.
Notes: ## follow the screen##

## Slide 12: MeS crystallization
The crystallinity of the metal sulphides is of utmost importance particularly when they are used in high-tech industrial processes (Bansal et al., 2013).
The factors determining crystallinity in sulphidogenic systems are not clear yet, although the crystallinity of biogenic ZnS was better than than abiogenic ZnS (Xu et al., 2016).
Mineral crystallinity is an attractive approach to achieving metal sulphide biological production in off-line sulphidogenic systems and to realizing the recovery of valuable resources from waste streams.
Sources:
Bansal et al., 2013. International Journal of Scientific Reports, 3, 1531.
Xu et al., 2016. Geochimica et Cosmochimica Acta, 180, 1-14.

## Slide 13
Sulphur conversion-based resource recovery: elemental sulphur recovery and reuse

## Slide 14: Elemental sulphur recovery
Elemental sulphur is also worth recovering and reusing with the assistance of a group of sulphur conversion-based bacteria, namely chemolithotrophic SOB.
SOB use O2 as the electron acceptor to oxidize sulphide to elemental sulphur. The basic principle for selective sulphur oxidation is to regulate the molar ratio of oxygen-to-sulphide (O/S) at approximately 0.7 (Lin et al., 2018).
Source: Lin et al., 2018. Water Research 143, 399-415.
Figure source: Book on Sulphur Removal and Recovery

## Slide 15: Effecting factor: DO control
DO control is a common strategy to reach the proper O/S ratio when the reactor is operated under a relatively stable sulphide concentration;
However, the dynamic DO concentration resulting from its continuous consumption causes difficulties in maintaining the desired O/S ratio (Janssen et al., 1998).
Source:
Janssen et al., 1998. Biotechnology and Bioengineering 60(2), 147-155.

## Slide 16: Effecting factor: ORP control
Oxidation-reduction potential (ORP), determined by both sulphide and DO concentrations, is a more feasible, alternative indicator for controlling selective sulphur oxidation.
Figure source: Water Environment Research, Vol 78, Number 4, pp. 397

## Slide 17: Example: THIOPAQ®
It has been applied for gas desulphurization for over 25 years (Paques, the Netherlands). This system consists of three parts: the sulphide absorber, the sulphide-oxidizing bioreactor and the sulphur settler.
https://equinox-eng.com/blog/2022/02/04/thiopaq-bio-desulphurization/
https://solarimpulse.com/solutions-explorer/thiopaq
Notes: First, the sulphide-containing gas stream contacts an alkaline solution in the absorber. Afterwards, the sulphide-containing liquid is transferred to a sulphide-oxidizing bioreactor where the sulphide is converted biologically to elemental sulphur under weak alkaline conditions (pH 8-9) by SOB, typically dominated by the haloalkaliphilic Thioalkalivibrio. Finally, the mixed liquid enters a settler to recover the elemental sulphur. In this process, over 90 % of the influent sulphide can be converted to elemental sulphur (Van den Bosch, 2008).

## Slide 18: Elemental sulphur reuse
The recovered elemental sulphur serves as a raw material for sulphuric acid, fertilizers and pesticide production.
In contrast to commercial crystalline sulphur, the sulphur produced from biological sulphide oxidation is characterized by high hydrophilicity and biological activity.
Figure source: Nature Food volume 4, pages442–444 (2023)
Notes: Biogenic elemental sulphur can stimulate sulphuric acid generation and dissolution of sulphide ores relative to chemical elemental sulphur during biological sulphide oxidation in the leaching process (Tichý et al., 1994).
Biogenic sulphur can be used directly as a fertilizer, which is demonstrated with an oil-bearing vegetable, canola. A 50 % increase in grain yield was observed after the addition of biogenic sulphur, outperforming the commercial elemental sulphur used in the same study (Cline et al., 2003).
The sulphur-limestone process using elemental sulphur to drive autotrophic denitrification for groundwater remediation has a low reaction rate due to the low solubility of sulphur.
Biogenic sulphur may overcome this drawback because its hydrophilicity would accelerate the mass transfer.

## Slide 19: Elemental sulphur reuse
Biogenic elemental sulphur can stimulate sulphuric acid generation and dissolution of sulphide ores relative to chemical elemental sulphur during biological sulphide oxidation in the leaching process (Tichý et al., 1994).
Biogenic sulphur can be used directly as a fertilizer, which is demonstrated with an oil-bearing vegetable, canola. A 50% increase in grain yield was observed after the addition of biogenic sulphur, outperforming the commercial elemental sulphur used in the same study (Cline et al., 2003).

## Slide 20: Elemental sulphur reuse
The sulphur-limestone process using elemental sulphur to drive autotrophic denitrification for groundwater remediation has a low reaction rate due to the low solubility of sulphur.
Biogenic sulphur may overcome this drawback because its hydrophilicity would accelerate the mass transfer.

## Slide 21
Sulphur conversion-based resource recovery: metabolic intermediate recovery

## Slide 22: Biohydrogen
High level of hydrogenase activity is often observed in SRB-enriched systems, especially in environments with low concentrations of sulphur.
H2 production during the breakdown of lactate from the SRB species.
Figure source: doi: 10.3389/fmicb.2019.01652
Notes: With formate as the sole electron donor, the highest H2 production rate of 0.6 mmol/lmedium/h was recorded with the mediation of Desulphovibrio vulgaris Hildenborough (Martins and Pereira, 2013). This production rate can significantly increase to 5 mmol/lmedium/h by using a sparging reactor to maintain a low H2 partial pressure (PH2) which facilitates the reaction thermodynamics (Martins et al., 2015). However, whether the energy recovered from the H2 production is equivalent to the gas supply for sparging is still unclear.
The electron transfer pathways of formate-driven H2 production by Desulphovibrio were proposed by Martins et al. (2016).
The direct electron transfer involving periplasmic enzymes ([NiFeSe] Hase) and the transmembrane electron transfer allow energy metabolism; however, the relative weights of these two pathways are unknown.
Conversely, H2 production by Desulphovibrio gigas occurs exclusively via the direct periplasmic enzyme route and transmembrane electron transfer is not involved at all. Desulphovibrio gigas and Desulphovibrio vulgaris are quite distinct in terms of number, type, and localization of hydrogenase, resulting in variations in their H2 production performance (0.26 mmol/l/h in Desulphovibrio vulgaris; 0.11 mmol/l/h in Desulphovibrio gigas).
Compared with Desulphovibrio vulgaris which contains a large number of hydrogenases, only two [NiFe] Hases are present in Desulphovibrio gigas: the energy-conserving hydrogenase (Ech) and the periplasmic HynAB-1 (Morais-Silva et al., 2013).
SRB have also been found to catalyze H2 production at the cathode of bioelectrochemical systems. A pure culture of Desulphovibrio vulgaris Hildenborough immobilized onto a carbon electrode can catalyze H2 production with methyl viologen as a redox mediator (Tatsumi et al., 1999), while a mediator-less microbial biocathode is more desirable for the stable operation of electrolysis systems.
A Desulphitobacterium-enriched culture without mediators at the cathode was proposed accordingly, achieving four times higher H2 production rate than that of the abiotic controls (Villano et al., 2011).
Furthermore, the capability of Desulphovibriocaledoniensis and Desulphovibrio paquesii to receive electrons directly from a graphite cathode for catalysing H2 production was demonstrated. Additional efforts are required for applying SRB for H2 production.

## Slide 23: Hydrocarbons
For the sulphate-reducing process, incomplete oxidizers usually outcompete complete oxidizers for substrates, such as intermediates of anaerobic degradation of organic matter (e.g. H2 and/or lactate), and incomplete oxidation becomes the dominant metabolic pathway.
This also results in more intermediate production during their metabolism.
  e.g. Production of aliphatic hydrocarbons of C10-C25 by Desulphovibrio with organics or fatty acids
https://www.sciencedirect.com/topics/earth-and-planetary-sciences/sulphate-reducer
Notes: n-C25-C35-alkanes could be the major product (up to 80 % of the total hydrocarbons) produced by Desulphovibrio desulphuricans, and CH3COO- and formate are simultaneously formed with fixation of CO2 (Bagaeva, 1998).
It has been hypothesized that this synthesis is initiated by formation of CH3COO- and formate through CO2 fixation. The produced micro-molecules are reduced to aldehydes, which further undergo aldol condensation elongating the carbon chain to produce hydrocarbons. Synthesis of hydrocarbons by Desulphovibrio desulphuricans depends largely on the medium composition and the volumetric ratio of H2 to CO2 (the optimum is 9:1) in a gaseous phase (Bagaeva, 2000). The supply of H2 is in favour of bacterial growth and synthesis of reduced products including hydrocarbons. The intracellular hydrocarbon synthesis potential of Desulphovibrio desulphuricans ranges from 0.8 to 2.25 % dry weight. Apart from Desulphovibrio desulphuricans, Desulphovibrio desulphuricans G20 has also been reported to extracellularly synthesize alkanes (Friedman and Rude, 2012). Overall, many obstacles remain to be conquered before SRB can be used as an economically viable biocatalyst for the industrial manufacture of ‘drop-in’ biofuels.

## Slide 24: Polyhydroxyalkanoates
The storage of polyhydroxyalkanoates (PHAs) in SRB has been investigated for their PHA synthesis ability in different saline water media.
Benzoate-grown Desulphonema magnum demonstrated the highest PHA content of 88% (wt./wt.) of cell dry matter, which is comparable to some of the best commercially applied organisms.
Figure source: Microb Ecol 85, 572–585 (2023).
Notes: The production cost of PHAs in fed-batch mode using waste materials could reach up to 3-5 USD/kgPHAs (Roland-Holst et al., 2013), which is much higher than that of oil-based plastics of approximately 1 USD/kgPHA (Salehizadeh and Van Loosdrecht, 2004). Most of the cost associated with the biosynthesis of PHAs is related to feedstock, aeration (if required), sterilization (maintaining a pure culture) and extraction of the PHAs. Optimistically, sharing the costs between wastewater treatment and PHA production would be an option when applying SRB-based technologies, for instance.
The PHA contents in Desulphobacterium autotrophicum, Desulphococcus multivorans, Desulphosarcina variabilis, and Desulphobotulus sapovorans were 11, 27, 22, and 43 % (wt./wt.) of the cell dry matter, respectively.